## Slide 1: Bryansk 2018
Выбор критерия для моделирования процесса накопления контактно-усталостных повреждений
в колёсах железнодорожного подвижного состава
Choice of criterion for modelling of process
of accumulation of rolling contact fatigue damage
in the railway wheels
IV scientific and technical workshop
COMPUTER SIMULATION IN RAILWAY TRANSPORT:
DYNAMICS, STRENGTH, WEAR
Sakalo V.I., Sakalo A.V.
Laboratory of Computational Mechanics,
Bryansk State Technical University

## Slide 2
Rolling contact fatigue
Rolling contact fatigue (RCF) is the process of accumulation of damage and progressing of the destruction of the surface layers of the material through variable contact loads, causing the spalling and shelling or cracks formation and a decrease of durability.
Defects of the wheels of freight cars, formed as a result of rolling contact fatigue

## Slide 3
Approaches to RCF assessment
There are two approaches to RCF assessment:
1) estimation of safety margin using the safety factor;
2) modelling of process of accumulation of RCF damage.
The first approach is used for estimation of safety margin in high cycle fatigue.
In the second approach the curves of RCF of the Weller's curves type are used. They are presented in the form typical for the low cycle fatigue
,
where σeq is the selected criterion of the contact strength; N is the number of cycles of variable stresses before RCF failure of a material; C, m are the material constants.
Nj
N
The accumulated damage in the i-th node is calculated as
,
where Ni(j) is number of cycles before RCF failure, when the value of criterion is ; n is the number of the contacts of the one radial cross-section of the wheel with the rail.

## Slide 4
RCF tests
Constructing RCF curves requires the solution of two problems – determination of the criterion value for the different load levels and the material constants.
Specimens in the form of rollers or discs with a diameter 30-40 mm of thickness 8-12 mm are typically used for RCF testing of materials (Fig. a). One roller is made of the wheel steel. Other roller is made of the rail steel. In some papers the roller made from rail steel is referred as a loading roller. The loading roller may also be made of high-strength steel or the alloy WC8 (the Russian steel grade) which contains W 92wt%, Co 8wt% and has hardness of 88 HRA. Specimen material in the contact area is in a state of plane strain. The stress state at the butt ends of the specimen is a plane stress so the thickness of the loading roller must be sufficient so the influence of the butt ends can be ignored.
To obtain the maximum contact pressure of about 2000 MPa it is necessary to apply the load of 9.16 kN when the specimen sizes are d = 40 mm, B = 8 mm. The load is decreased by decreasing the contact length B (Fig. a). In this case the loading roller of the length B = 3 mm (Fig. b) or the roller with width of the rolling surface 3-4 mm (Fig. c) is used. The rollers with the toroidal surface of rolling are also used (Fig. d).
(d)
(c)
(b)
(a)
B
d
3 mm
R

## Slide 5
Criterion of maximum contact pressure
In the common practice it is accepted to construct the RCF curves as diagram: the number of cycles N before the appearance of the fatigue failure vs. the maximum contact pressure p0. The maximum contact pressure is taken as the criterion of the contact fatigue.
There are several reasons why it cannot be used as a criterion for modelling of the processes of accumulation of RCF damage.
1) Use of this criterion does not take into account the creeps, spin and tangential forces distributed over the contact surface and arising during rolling of the wheels when braking or traction are applied. These factors significantly influence on the stress state.
2) The criterion cannot consider the residual stresses in the subcontact layer of the material.
3) The RCF tests are done under the high contact pressures up to 3500 MPa. This gives rise to plastic deformations in the subcontact layer which leads to a change of geometry of the contact surfaces, and a subsequent change of the contact pressure distribution. In this reason in tests using a loading roller with toroidal tread the maximum pressure is reduced by as much as 1.5 times during test.
R19,3
R18
R20
1
2
Finite element (FE) model:
1 – toroidal loading roller;
2 – specimen
The cross-section of the trough, which formed due to rolling of the loading roller on specimen; displacements along the y axis was increased by 20 times
The contact pressure distribution under load of 496 N:
a – during initial rolling; b – during repeated rolling
(a)
(b)
Solving of rolling contact problem in the elastoplastic formulation

## Slide 6
Criterion of amplitude of maximum shear stress
The simplest criterion used in simulation of RCF damage accumulation is the maximum shear stress τmax.
Its suitability as a criterion is obvious when taking into account the dominant idea of the nature of fatigue failure: due to shifts of material on the planes of action of the maximum shear stresses. Through such shifts, the material becomes friable, and microcracks are formed. Repetition of this process leads to crack growth.
The criterion allows taking into account the stresses caused by normal and tangential forces in the contact.
The drawback of this criterion is that it does not take into account the hydrostatic pressure and residual stresses.
The favorable conditions for the formation and development of cracks are created when there is multiaxial tension in the material. The formation of cracks is more difficult with multiaxial compression.
A
x
O
z
y
i
j
Loading path
b
a
Contact patch
An analysis of the distribution of the values of the τmax criterion in the region adjacent to the elliptical contact patch was carried out using FE model of the parallelepiped. It was made of eight-node finite elements with rib sizes of 1 mm. The vertical forces were applied in the nodes located on the surface of the contact patch. Their values were determined in accordance with the law of pressure distribution
where a, b are semiaxises of contact ellipse; p0 – maximum pressure.
The value of the criterion was determined for the nodes of the plane FE mesh A, which was dragged through the subcontact region along the Oz axis in steps equal to the length of the rib of the finite element. The value of the maximum shear stress was determined for each position j of the node i occupied by moving the mesh
The value of the criterion for node i of the plane FE mesh was calculated as the half of difference between the maximum and minimum value τmax obtained at the nodes j

## Slide 7
Criterion of amplitude of maximum shear stress
1
2
3
4
5
6
1
2
3
4
5
6
1
2
3
4
5
6
1
2
3
4
5
6
The normal force was assumed equal to 120 kN and the maximum pressure was 1000 MPa for all variants. The eccentricity of the contact ellipse was varied, where β = b/a. Also the friction coefficient f was varied.
The isolines of the values of the criterion in the area of elliptical contact
e = 0.2; f = 0.0; Maximum value of is 163 MPa
e = 0.2; f = 0.3; Maximum value of is 174 MPa
e = 0.9; f = 0.0; Maximum value of is 170 MPa
e = 0.9; f = 0.3; Maximum value of is 181 MPa

## Slide 8
Dang Van criterion
The Dang Van criterion is represented by two inequalities
(a)
(b)
(1)
were τa(t) is time-depended value of shear stress at the specified material point and in the specified shear plane through this point –
so called shear stress “amplitude”. The value τa(t) is calculated as the difference between the current magnitude at time t of the shear stress in the specified plane and it middle magnitude during one cycle;
is time-depended value of hydrostatic stress at the same material point;
are normal stresses at the same point;
αDV is Dang Van coefficient;
τe is fatigue limit of the material in pure shear.
The criterion is represented by a diagram in the form of two inclined lines corresponding to inequalities (1a) and (1b). The hydrostatic pressure is plotted along the abscissa axis and the "shear stress amplitude" along the ordinate axis, which can be either positive or negative (see Fig.)
FATIGUE
τe
τa
σh
τe/αDV
-τe
A
B
τa = τe - αDVσh
τa = αDVσh - τe
FATIGUE
NO FATIGUE
NO FATIGUE
The Dang Van diagram

## Slide 9
τe
τa
O
D
C
B
A
τa
σh
σh
φ
φ
τe/αDV
E°
Dang Van criterion
The Dang Van coefficient is equal to the tangent of the slope angle of the cyclic fatigue diagram φ (see Fig.) Then the criterion is numerically equal to the length of the OC segment cut off by the line passing through point A with coordinates σh, τa(t) running parallel to the inclined line of the diagram. The ratio τa(t)/OC can be considered as a factor of safety of cyclic strength, therefore the states represented by points A and B are equally dangerous.
An inclined straight line passing through the point D cuts off a short segment on the axis τa(t), the safety factor takes a large value. If the straight line crosses the axis τa(t) at a point with a negative criterion value, the criterion is assumed to be zero (the line passing through the point E). If the absolute value of the shear stress τa(t) is used in the calculations, only the upper part of the diagram can be used.
Then the Dang Van criterion can be represented in the form
The quantities τa(t) and σh(t) vary in time. In calculations using FE schemes the time is transformed into the coordinates of the points i occupied by the node as it passes through the region adjacent to the contact.
In order to simplify calculations τa(t) at the point, instead of the tangential stress at a certain point of the material and in a certain plane passing through this point, the maximum tangential stress is used.
Then the average maximum shear stress is equal
where n is number of positions of the node.
The amplitude value of the shear stress is found as
The dependence is used to determine the Dang Van coefficient, where σe is the fatigue limit of the wheel material under a uniaxial stress state. The recommended value of the coefficient is 0.38.
(2)
(3)
(4)

## Slide 10
Dang Van criterion
The normal force was assumed equal to 120 kN and the maximum pressure was 1000 MPa for all variants. The eccentricity of the contact ellipse was varied, where β = b/a. Also the friction coefficient f was varied.
The results of calculation of the criterion in the area of elliptical contact
1
2
3
4
5
6
The distribution of values of the criterion on the contact surface (xOz plane):
e = 0.2; a = 7.65 mm; b = 7.49 mm
(a)
(b)
(c)
The distribution of values of the criterion in the subcontact area (yOz plane):
e = 0.2; a = 7.65 mm; b = 7.49 mm
The isolines of the values of criterion in the area of elliptical contact for the plane mesh drawn along the axis Oz through the region adjacent to the contact:
e = 0.2; a = 7.65 mm; b = 7.49 mm;
1-6 is number of isoline
The negative values are obtained for all nodes located at the contact patch, so they were assumed to be zero.
The zero values of the criterion are obtained for the entire area located below the contact patch, as can be seen from the picture of isolines for nodes located in the yOz plane (Fig.b). Non-zero values are obtained outside the contact patch. The picture of isolines for the plane mesh that is drawn through the subcontact area is shown in Fig.c. The maximum value of the criterion 145 MPa are obtained for the node located on the Oy axis at a depth of 2 mm.

## Slide 11
Sines criterion
The Sines criterion is described by the following equation
where P1, P2, P3 are amplitudes of the alternating principle stresses;
Sx, Sy, Sz are normal components of mean stress;
A is material constant proportional to reversed fatigue strength;
α is material constant, which gives variation of the permissible range of stress with static stress.
These criteria contain a component of the type
associated with the potential energy of the change in shape. It represents doubled modulus of the sum of the principal tangential stresses
This component, multiplied by one or another coefficient, represents the variable component of the cycle of stresses.
The hydrostatic pressure represents a constant component of stresses. It associated with the potential energy of the change in volume.
The results of calculation of the criterion in the area of elliptical contact
1
2
3
4
5
6
1
2
3
4
1
2
3
4
5
6
1
2
3
4
1
2
3
4
5
6
1
2
3
4
The normal force was assumed equal to 120 kN and the maximum pressure was 1000 MPa for all variants. The eccentricity of the contact ellipse was varied, where β = b/a. Also the friction coefficient f was varied.
The zero values of the criterion are obtained on the contact surface inside contact patch and for the entire area located below the contact patch.
e = 0.2; f = 0.0;
Maximum value is 42 MPa
e = 0.2; f = 0.17;
Maximum value is 62 MPa
e = 0.2; f = 0.3;
Maximum value is 82 MPa

## Slide 12
Criterion of specific potential energy of deformation
We propose the RCF criterion, which obtained on the basis of the two components of the specific strain energy.
The specific strain energy is used as a criterion for evaluating the strength at a point of a solid body. The criterion theories of strength are constructed according to the following scheme. An expression for the specific strain energy for a multiaxial stress state is written. A uniaxial stress state, which equivalent to the multiaxial stress state is defined. The expressions for the specific strain energies for these two states are equated and expressions for the criterion are obtaining.
The specific strain energy in the case of the multiaxial stress state is equal
where σ1, σ2, σ3 are the principal stresses; Е is tensile modulus; ν is Poisson's ratio.
In case of the uniaxial stress state
where σtens is normal stress under uniaxial tension.
Equating expressions (1) and (2), we obtain the criterion
The stress state at the point can be divided into two states: one causes a change of the shape of the selected element; the other causes a change of its volume. The second state is represented by three components equal to the hydrostatic pressure
In accordance with this division, the energy of change of the shape is
and energy of change of the volume is
By using this approach, taking into account that in the case of all-round compression the bodies are not destroyed, Mises excluded the energy of change of the volume from consideration and obtained the criterion that takes into account the energy of change of the shape.
(1)
(2)
(3)
(4)
(5)
(6)

## Slide 13
Criterion of specific potential energy of deformation
The expression for the specific strain energy as the sum of the energy of change of the shape (5) and the energy of change of the volume (6) for the multiaxial stress state and for the uniaxial stress state is written. The energy of change of the volume is considered as positive if the volume of the element increases. With negative hydrostatic pressure the volume of the element decreases, the energy of change of the volume is taken with the minus sign.
The obtained expressions are equated and the uniaxial stress state, which equivalent to the multiaxial stress state is determined.
The RCF criterion is obtained for a cycle of the equivalent uniaxial stress state.
The specific strain energy for the multiaxial stress state is
For the uniaxial stress state it is equal
Equating expressions (7) and (8), we obtain
If the left side of the equality (9) is positive then the equivalent stress is
If the left side of equality (9) is negative, it is assumed to be equal to
(7)
(8)
(9)
(10)
(11)

## Slide 14
The introduction of the coefficient ψσ makes it possible to express the parameters of the cycle, which is represented by the point K through the parameter of the symmetric cycle σ-1. Similarly, the parameters of the cycle, which is represented by the point M can be expressed in terms of the parameter σ’-1 of the equivalent symmetric cycle.
Then the ratio can be regarded as a factor of safety, and
as a criterion of fatigue.
Criterion of specific potential energy of deformation
The criterion theory of strength makes it possible to find the uniaxial stress state, which equivalent to the multiaxial stress state and then calculate the fatigue for the uniaxial stress state. The diagram of limit stress (Haigh diagram) is used in fatigue calculations. Serensen and Kinasoshvili proposed an approximation of this diagram (see Fig.) The segment that limits strength due to fatigue failure is constructed by the results of two tests. The tests with a symmetrical cycle allow obtaining the limit of endurance σ-1. It is represented by point A in the diagram. The tests in the pulsation cycle give the value of the endurance limit σ0, which is represented by a point C with coordinates σm = σ0/2 and σa = σ0/2. Through the points A and C a straight line is drawn that approximates the limiting curve. The tangent of the slope of this line is
It is called the coefficient of sensitivity of material to the asymmetry of the cycle. The values of the coefficient depending on the ultimate strength σu of the material are shown in the Table.
(12)
(13)
σu, MPa | 350-550 | 520-750 | 700-1000 | 1000-1200 | 1200-1400
Ψσ | 0 | 0.05 | 0.1 | 0.2 | 0.25
M
σys
0.5σ0
45º
O
A
N
C
K
L
σa
σm
σ´-1
σ-1
0.5σ0
Approximated Serensen-Kinasoshvili diagram

## Slide 15
Criterion of specific potential energy of deformation
The normal force was assumed equal to 120 kN and the maximum pressure was 1000 MPa for all variants. The eccentricity of the contact ellipse was varied, where β = b/a. Also the friction coefficient f was varied.
The results of calculation of the criterion in the area of elliptical contact
0
1
2
4
3
2
1
0
1
2
3
4
2
1
0
1
2
3
4
2
1
4
5
6
3
2
2
1
4
5
6
3
2
1
4
5
6
3
2
1
e = 0.2; f = 0.0
The isolines of the values of the equivalent stress σeq in the plane yOz in the area of the Hertzian contact are shown below. The price of the isoline is 255.7 MPa. At a depth of up to 2 mm the equivalent stresses are compressive. The isolines of 1-4 numbers are located in this area. The equivalent stresses are positive in the points located below. The greatest negative equivalent stress in the point located at the contact surface is -1240 MPa, and the greatest tensile stress in the point located at a depth of 5 mm is 550 MPa.
The lines for two values of the friction coefficient f = 0.17 and f = 0.3 shows the same maximum order of isolines – the seventh, but the price of the isoline is different. The maximum value of the positive equivalent stress for f = 0.17 is 560 MPa. The point with the maximum positive stress of 650 MPa for f = 0.3 is located on the contact surface.
e = 0.2; f = 0.17
e = 0.2; f = 0.3
The isolines of the values of the criterion σU in the plane mesh A are shown below. The highest values of the criterion are obtained for points located on the contact surface. The maximum values of the criterion are 700; 774 and 870 MPa, respectively, at values of the friction coefficient f equal to 0; 0.17 and 0.3.
e = 0.2; f = 0.0
e = 0.2; f = 0.17
e = 0.2; f = 0.3

## Slide 16
z
y
x
R 19.3
R 18
R 20
1
2
The results of RCF tests
The results from experimental tests using specimens of wheel steel castings were used to generate RCF curves. These tests were done at the Railway Research Institute (Russia). The experimental castings 6, 2 and 9 corresponded to the carbon content of steel grades 2, L and T respectively (Table 1).
The test specimens were cut at a distance of 10 mm from the rolling surface of the wheel. The cylindrical specimens of diameter 40 mm were used. The toroidal roller of the diameter of 38.6 mm with a radius of the torus 18 mm made of hard alloy WC8 was used as the loading roller (Fig.1). The speed of rotation of the specimen was 1500 rpm. The specimens were rolling without sliding. The oil I-20 was applied to the rolling surfaces. The tests were carried out on five load levels. From 1 to 5 samples were tested at each load level. The test results are shown in Table 2.
The stress-strain state of the specimens was analyzed by the FE method. The FE meshes of the fragments of the wheel steel specimen and the loading roller are shown in Fig.2. They had dimensions on the x and z axes of 3.15 mm, on the y axis of 1.5 mm. The finite elements with eight nodes and dimensions of the ribs along the x and z axes of 0.075 mm and 0.1 mm along the y axis were used.
The rollers had dimensions: the radius of the specimen of the wheel steel is 20 mm, the radius of the loading roller is 19.3 mm and the radius of the torus is 18 mm.
The loading roller material had following parameters: 5.9·1011 Pa for the tensile modulus and 0.202 for the Poisson's ratio.
The wheel steel specimens material had following parameters: 2.0·1011 Pa for the tensile modulus and 0.3 for the Poisson's ratio.
The FE model of the wheel steel specimen had 26 896 nodes. The FE model of the loading roller had 11 767 nodes. The number of the finite elements was 24 000 and 9 600 respectively.
The rolling contact problem was solved in the elastoplastic formulation.
Fig.1. Scheme of RCF test:
1 – loading roller;
2 – specimen of the steel
Fig.2. FE models of the fragments
of the wheel steel specimen (1)
and loading roller (2)
Number of the casting | The carbon content, wt% | Hardness, HB
6 | 0.57 | 269
2 | 0.54 | 295
9 | 0.73 | 322
Load, N | The durability, cycles∙105 |  | 
 | Casting 6 | Casting 2 | Casting 9
120 | 8.71 | 11.73 | 18.90
300 | 5.12 | 5.86 | 9.14
600 | 2.82 | 3.21 | 5.78
900 | 2.90 | 2.80 | 3.87
1200 | 1.89 | 2.16 | 2.91
Table 2
Table 1

## Slide 17
The construction of RCF curves
The values for each of the four criteria for the steels of the experimental castings are obtained. These values, for example, for specific strain energy for the steel of experimental casting 6 are presented in Table below.
Load, N | 120 | 300 | 600 | 900 | 1200
σU, MPa | 696 | 986 | 1144 | 1260 | 1320
The durability, cycles∙105 | 8.71 | 5.12 | 2.82 | 2.9 | 1.89
The coefficients C and m in the dependence
are obtained in results of approximation by least square method.
Fig.1. RCF curve for criterion of specific strain energy
for the steel of experimental casting 6
Fig.2. RCF curves for criterion of
amplitude of maximum shear stress
Fig.5. RCF curves for criterion of
specific strain energy
Fig.3. RCF curves for Dang Van
criterion
Fig.4. RCF curves for Sines criterion

## Slide 18
1
3
1
4
1
6
1
2
3
4
5
6
The results of modelling of accumulation of RCF damage
1
2
3
4
5
6
1
2
3
4
5
6
1
Fig.2. The criterion of amplitude of maximum shear
stress: the traveled distance is 5600 km; the depth of
locating of the point with the biggest damage is 2 mm
Fig.3. The Dang Van criterion: the traveled distance is
8000 km; the depth of locating of the point
with the biggest damage is 2 mm
Fig.5. The criterion of specific strain energy: the traveled
distance is 23000 km; the point with the biggest
damage is located on the contact surface
Fig.4. The Sines criterion: the traveled distance is
14700 km; the depth of locating of the point
with the biggest damage is 3 mm
Fig.1. FE mesh of the plane radial cross-section of the
fragment of the wheel
The accumulated damage is determined for the points of the plane radial cross-section of the fragment of the wheel. The part of this section is represented by a plane FE mesh for the nodes of which the process of accumulation of damage is simulated (Fig.1).
Each time the cross-section passes through the area adjacent to the contact, increments of accumulated damage are obtained for the nodes of the mesh. This radial cross-section with isolines of accumulated damage for wheel with worn profile made of steel of the casting 2 is shown in Figs. 2-5.

## Slide 19: Thank you for attention!
Выбор критерия для моделирования процесса накопления контактно-усталостных повреждений
в колёсах железнодорожного подвижного состава
Choice of criterion for modelling of process
of accumulation of rolling contact fatigue damage
in the railway wheels
IV scientific and technical workshop
COMPUTER SIMULATION IN RAILWAY TRANSPORT:
DYNAMICS, STRENGTH, WEAR
Sakalo V.I., Sakalo A.V.
Laboratory of Computational Mechanics,
Bryansk State Technical University