## Slide 1: Crack propagation simulation in railway rolling stock axles
Volokhov G.M.,
Doctor of Engineering,
Knyazev D.A.,
Timakov M.V.
VNIKTI
temev@mail.ru
Notes: <number>

## Slide 2: Durability concept
2
VNIKTI
Durability is a period of time during which a technical device, building, facility or system can perform its functions despite obtained damages.
temev@mail.ru
Notes: <number>

## Slide 3: Subject of Research
3
VNIKTI
A solid and hollow axle with a pressed-on vibrator head fixed in a technological hub
temev@mail.ru
Notes: <number>

## Slide 4: Research Area
4
VNIKTI
According to results of calculations and tests the most loaded area is the axle seat
temev@mail.ru
Notes: <number>

## Slide 5: Determining an initial and finite crack depth
5
VNIKTI
An initial crack depth is determined using facilities
A finite crack depth is determined as a result of an object failure
temev@mail.ru
Notes: <number>

## Slide 6: Crack depth (length) measurement
6
VNIKTI
temev@mail.ru
Notes: <number>

## Slide 7
7
VNIKTI
Experimental procedure
temev@mail.ru
Notes: <number>

## Slide 8: A research theoretical basis is Paris formula
8
VNIKTI
Crack propagation rate is in proportion to the degree m of the stress intensity factor
The stress intensity factor is in proportion to the product of a stress amplitude and the square root of the crack depth
temev@mail.ru
Notes: <number>

## Slide 9
9
ВНИКТИ
temev@mail.ru
Paris formula correction in respect to the subject of research
For solid axle:
For hollow axle:
Notes: <number>

## Slide 10
10
VNIKTI
Selection of parameters С and m using the least square method
For solid axle:
For hollow axle:
temev@mail.ru
Notes: <number>

## Slide 11
11
VNIKTI
Selection of parameters С and m using the least square method
temev@mail.ru
Notes: <number>

## Slide 12
12
VNIKTI
Approximation result
m=3.20
C=2.7×10-14
m=3.24
C=2.8×10-14
temev@mail.ru
Notes: <number>

## Slide 13
13
VNIKTI
Load bank
temev@mail.ru
Notes: <number>

## Slide 14
14
VNIKTI
Durability
For solid axle: l0=1,8 mm l=100 mm N=86 000 000 cycles L=284 000 km(Ø1050mm)
For hollow axle: l0=1,8 mm l=100 mm N=78 000 000 cycles
L=257 000 km(Ø1050mm)
temev@mail.ru
Notes: <number>

## Slide 15: Thank you for attention!
15
VNIKTI
temev@mail.ru
Notes: <number>